Jun. 2019
18063 binary compounds
56102 ternary compounds

No compound is available for Rn, transition metals with atomic number 104 to 112, actinide with atomic number 95 to 103, and Po, At, Fr, and Ra, i .e. data are available for 89 elements in the periodic table.
Some compositions are repeated due to the polymorphism (materials with exactly the same composition but different crystal structures). In such a situation the most stable structure is considered. After removing the polymorphs the number of binary compounds is 10743 and the number of ternary compounds is 42156.

To make the database for ML, we consider only the most stable binary and ternary compounds. The formation energy of compounds can be calculated with a heuristic formula. To do this for a ternary compound, we need the two binary compounds that can form the ternary compound. In this case, the ternary compound’s formation energy can be calculated by the composition-weighted average of corresponding binary compound formation energies. For example:

(w1 = 0.634) Bi13O20 (Ef = -1.608) + (w2 = 0.375) Sm2O3 (Ef = -3.879) → Sm3Bi5O12
The DFT calculated formation energy for this compound is -2.460 eV. The formation energy calculated by the heuristic formula is -2.476 eV.

For some ternary compounds, there is more that one combination of binary compounds. For example:

Y(Bi3O5)4, (w = 0.923) Bi13O20 (Ef = -1.608) + (w = 0.076) Y2O3 (Ef = -3.989),
EDFT = -1.761, Eheuristic = -1.787
Y(Bi3O5)4, 0.916, Bi25O38, -1.605, 0.076, Y2O3, -3.989,
-1.761, -1.773
Y(Bi3O5)4, 0.916, Bi25O38, -1.605, 0.091, YO2, -3.010,
-1.761, -1.745
Y(Bi3O5)4, 0.909, Bi2O3, -1.654, 0.091, YO2, -3.010,
-1.761, -1.777
Y(Bi3O5)4, 0.932, Bi16O25, -1.585, 0.076, Y2O3, -3.989,
-1.761, -1.779
Y(Bi3O5)4, 0.952, Bi4O7, -1.583, 0.048, Y5Bi3, -0.726,
-1.761, -1.542
These data can be found in the “ternaries-from-binaries” file.
49680 combinations of binary compounds can be made from the binary and ternary compounds available in MPD. Not all the combinations of binary compounds give a good heuristic formation energy. In the above-mentioned the first 5 combinations give an reasonable accurate heuristic formation energies, whereas the error in the formation energy of the one is about 12%.
We want to do a two-step ML.
Step1:
Training:
In the first step, we want to understand when the heuristic formula gives an accurate formation energy. We don’t have criterion for this accuracy. We can say the heuristic formation energy to be accurate if its value is less that 10% different from the DFT formation energy.
First we consider all the most stable ternary compounds in the MP database (42156) and find all the combinations that two ternary compounds from the MP database (10743) can give the formation energy of these ternary compounds. It is possible to calculate the heuristic formation energies for 21348 of 42156 ternary compounds available in MPD.
This results in a dataset with 49680 entries that can be used for the training (33850 as class 0 and 15830 as class 1 for 10% accuracy; 39520 as class 0 and 10160 as class 1 for 5% accuracy). It should be noted that some ternaries cannot be made from binaries and some ternaries can be made from different combinations of binaries.
The descriptors to train the system can be as follows:

For the ternary compound (37):
1- Heuristic formation energy (1)
2- Average of: Pauling electronegativity, group, row, mas, ionic radius, electron affinity, first ionization energy, vdw radius (8)
Ratio of properties of elements to the average value for
3- Electronegativity (3)
4- Group (3)
5- Row (3)
6- Mass (3)
7- Ionic radius (3)
8- Electron affinity (3)
9- First ionization energy (3)
10- vdW radius (3)
11- Orbital fraction of valence electrons (4 (s, p, d, and f))

For each binary compound (40):
1- Weight
2- Formation energy
3- Ratio of anion to cation
4- Ratio of the cation to ternary
5- Ratio of anion to ternary
6- Average of: Pauling electronegativity, group, row, mas, ionic radius, electron affinity, first ionization energy, vdw radius (8)
7- Absolute difference: Pauling electronegativity, group, row, mass, ionic radius, electron affinity, first ionization energy, vdw radius (7)
8- Difference: group, row, mass, ionic radius, electron affinity, first ionization energy, vdw radius (8)
9- Ratio cation to antion: group, row, mass, ionic radius, electron affinity, first ionization energy, vdw radius (8)
10- Orbital fraction of valence electrons (4 (s, p, d, and f))
11- Oxidation states of constituent elements in binary/Oxidation states of the same element in ternary (2), only for charge-neutral compounds

Classification:
The main goal of step 1 is to increase the data for the second step. It is possible to make some ternary compounds (by combining two binaries from the MP-DB) that do not exist in the MPDB. That means that we can calculate the heuristic formation energy but the DFT formation energy is not known. The trained system can classify these heuristic formation energy as accurate or not accurate.
The number of ternary compounds that we have the heuristic formation energy but the DFT formation energy is not known is depends of the total number of possible ternary compounds. The total number of possible ternary compounds with the formula AxByCy (x, y, z <8) is about 5000000. We cannot handle this number of compounds. We might try ternary compounds with smaller number of x, y, and z (x, y, z <4). After considering some chemical rules the total number of ternary compounds with AxByCy (x, y, z <4) formula is 502448.
The heuristic formation energy of 262200 of these 502448 compounds can be calculated form the binary compounds available in the MPD. For 7913 of these 262200 compounds, DFT formation energies are known from the MPD. That means that we have the heuristic formation energies for 254287 ternary compounds but we do not know if their heuristic formation energies are accurate or not (not classified). For these compounds, a dataset with 420152 entries can be formed.
Classification with 10% accuracy:
After classification, these entries are classified by the trained NN and 349122 of them are “not accurate”, whereas 71030 of them are classified as “accurate” (corresponding to 56591 ternary compounds). The latter will be used for the training of the NN for the second step.
Classification with 5% accuracy:
After classification, these entries are classified by the trained NN and 391437 of them are “not accurate”, whereas 28715 of them are classified as “accurate” (corresponding to 24466 ternary compounds). The latter will be used for the training of the NN for the second step.

Step 2:
Training:
Based on 10% accuracy
In addition to all ternaries with known DFT formation energies (42155 ternaries (one compound which contain He is removed)), those entries that are classified as 1 ( 71030 entries for 56591 ternary compounds) are used for the training of the NN for the second step. It should be mentioned that in this stage some compounds that are classified as 1 are repeated (71030-56591=14439). For these 14439 compounds the average of formation energies are calculated as the heuristic formation energy. That means, (42155+56591=)98746 entries for training of the second step.
If we want to have the validation step, then 6231 compounds with x,y,z<4 which their DFT formation energy is available but the heuristic formula does not predict the formation energy accurately are removed from 42155 ternaries (42155-6231=35924). That means total entries for training will be (35924+56591=)92515.

Based on 5% accuracy
In addition to all ternaries with known DFT formation energy (42155 ternaries (one compound which contain He is removed)), those entries that are classified as 1 ( 28715 entries for 24466 ternary compounds are used for the training of the NN for the second step. It should be mentioned that in this stage some compounds that are classified as 1 are repeated (28715- 24466= 4249). For these 4249 compounds the average of formation energies are calculated as the heuristic formation energy. That means, (42155+24466=)66621 entries for training of the second step.
If we want to have the validation step, then 7601 compounds with x,y,z<4 which their DFT formation energy is available but the heuristic formula does not predict the formation energy accurately are removed from 42155 ternaries(42155-7601=34554). That means total entries for training will be (34554+24466=)59020.
It should be noted that in this step the features are merely from the ternary compounds since we do not know the binary compounds that can make the ternary compounds.
Features (37):
1- Average of: Pauling electronegativity, group, row, mas, ionic radius, electron affinity, first ionization energy, vdw radius (8)
Ratio of properties of elements to the average value for
2- Electronegativity (3)
3- Group (3)
4- Row (3)
5- Mass (3)
6- Ionic radius (3)
7- Electron affinity (3)
8- First ionization energy (3)
9- vdW radius (3)
10- Orbital fraction of valence electrons (4 (s, p, d, and f))
11- Heuristic formation energy (1)
** The model can be trained only with 25971 entries for which the heuristic formula predict an accurate formation energy.

Regression:
Based on 10% accuracy
The ternary compounds that their formation energy should be predicted (after the model is trained) include the ternary compounds AxByCy (x, y, z <4) that their heuristic formation energies are not classified as “accurate” (197696 ternary compounds) and those that the heuristic formation energies cannot be calculated (240248) from the binary compounds available in the MPD. In total 437944 ternary compounds for which the formation energy should be predicted.

Based on 5% accuracy
The ternary compounds that their formation energy should be predicted (after the model is trained) include the ternary compounds AxByCy (x, y, z <4) that their heuristic formation energies are not classified as “accurate” (229821 ternary compounds) and those that the heuristic formation energies cannot be calculated (240248) from the binary compounds available in the MPD. In total 470069 ternary compounds for which the formation energy should be predicted.

Validation:
Based on 10% accuracy
For validation, we used the ternary compounds that their DFT formation energy is available but the heuristic formula does not predict the formation energy accurately (10487 compounds with class 0 that is used for training of the step 1). If we limit our test to those ternaries with x, y, and z smaller than 4, then the number decreases to 6231.

Based on 5% accuracy
For validation, we used the ternary compounds that their DFT formation energy is available but the heuristic formula does not predict the formation energy accurately (13630 compounds with class 0 that is used for training of the step 1). If we limit our test to those ternaries with x, y, and z smaller than 4, then the number decreases to 7601.